# Tel: 01522 787187

# Email: ROOSEMOTORSPORT@aol.com

# ROOSEMOTORSPORT PERFORMANCE SILICONE HOSES

## RETAIL

## Straight Hose x 1m (3’3”) long

Retail			     Retail			      Retail				                                           Standard      		 Flurolined                      High Temperature

SPS                                           FLPS                                   HTNS

Bore mm	Wall Size

6.0 mm	3.0 mm	                13.90			     29.78			     17.56

8.0 mm	3.0 mm	                14.42			     31.31			     17.94

10.0 mm	3.0 mm	                14.96			     33.60			     18.70

13.0 mm	3.0 mm	                17.10			     38.18			     21.38

16.0 mm	4.5 mm	                19.24			     42.77			     25.57

19.0 mm	4.5 mm	                20.31			     45.82			     26.73

22.0 mm	4.5 mm	                20.84			     49.64			     29.02

25.0 mm	4.5 mm	                21.38			     51.93			     34.36

28.0 mm	4.5 mm	                22.46			     55.75			     36.66

32.0 mm	4.5 mm	                23.78			     58.04			     38.18

35.0 mm	4.5 mm	                25.66			     62.62			     42.77

38.0 mm	4.5 mm	                27.80			     68.73			     45.06

45.0 mm	4.5 mm	                32.60			     76.37			     51.17

51.0 mm	4.5 mm	                37.42			     84.01			     57.28

54.0 mm	4.5 mm	                38.49			     87.83			     60.33

57.0 mm	4.5 mm	                39.56			     91.65			     64.91

60.0 mm	4.5 mm	                41.70			     96.23			     67.97

63.0 mm	4.5 mm	                42.77			   100.81		                    71.02

70.0 mm	6.0 mm	                48.11			   109.98		                    89.35

76.0 mm	6.0 mm	                53.46			   122.20			     95.46

102.0mm	6.0mm	                80.19			   160.38	             	                  109.98

### All Prices Include VAT

Operation	       Application

SPS : Standard Polyester Silicone                         -60 degree’s C to +180 degree’s C                                   Water and air

FLPS : Flurolined Polyester Silicone                     -60 degree’s C to +180 degree’s C	   Fuel and oil resistant

HTNS : High Temperature Nomex Silicone          -60 degree’s C to +240 degree’s C	      Turbo chargers

Standard Colours : Blue. Red

Colour options : Black. Yellow. Metalic Silver

Size Tolerance : + or – 0.5mm